Modelling of the mechanical loading effects on the effective diffusive behaviour of polymer matrix composites

D. Gueribiz1, F. Jacquemin2*, M. Rahmani1, S. Fréour2,  K. Loucif3

1 Département de Génie Mécanique, Université Amar Telidji Laghouat, Algérie.

2 GeM – UMR CNRS 6183, Université de Nantes, France.

3 Laboratoire des matériaux non métalliques, Université Ferhat Abbas Sétif, Algérie.

Abstract 

In this study, the effect of a mechanical loading on the diffusion process in a polymer matrix composite is discussed. The application of an external loading is expected to modify the microstructure of the material and causes change in effective diffusive behaviour as the diffusion in the polymer matrix is dependent on the free volume. On the basis of the free volume theory, the mechanical problem imposed on the representative volume element (RVE) is solved and then the volume fraction of free volume is determined. The effect of external mechanical loading on the moisture content and diffusion coefficient was first examined and finally the corresponding local stresses in the RVE are calculated.

1. Introduction

The study of transport phenomena in polymers is often based on the free volume theory (Crank and Park, 1968, Fahmy and Hurt, 1980). The free volume Vf is defined as the difference between the volume of the specimen Vm and the actual volume V0 occupied by the constitutive molecules:

Vf=Vm−V0	(1)

Inspired by the VTF equation (Vogel - Tammann - Fulcher), Doolittle (1951) proposed an empirical equation that describes the viscosity η as a function of the free volume fractionvf:

ln(η)=a+bvf	(2)

where a and b are constants (b is close to 1), the fraction of free volume is defined as follows:

vf=Vm−V0Vm=VfVm	(3)

A physical interpretation is given by Cohen and Turnbull (1959) considering that the different segments of chains are initially blocked by theirs neighbours and need a critical free volume to move. Without crossing barrier energy, the movement of atoms results from a redistribution of excess volume. The structure is rearranged by a diffusion mechanism mainly due to jumps of atoms in the free spaces created. The jumps are only possible if the volume cavity is greater than a critical volume. In this theory, a probability P(V*) is defined to find a cavity of size V*. For liquid with molecules of the same size, P(V*) is defined as:

P(V)=Aexp(−γVVf)	(4)

where A is a constant,  is a numerical parameter of unity order. The Product V* is considered as a measure of the minimum size for a cavity relative to a displacement  of the diffusion. This distribution model is based on several assumptions:

1 - The diffusion process occurs due to a redistribution of free volume in the matrix.

2 - The redistribution of free volume does not change the energy system.

3 - The diffusion process occurs when the free volume exceeds the critical size V* for the cavity.

4 - The diffusion is directly proportional to the probability P(V*) to find a cavity of volume greater or equal to V* adjacent to the diffusive molecule.

On the basis of Cohen and Turnbull (1959) assumptions, Fujita (1961) proposes a relationship between the diffusion coefficient D and the free volume fraction expressed as:

ln(DRT)=ln(Ad)−Bdv0f	(5)

where v0f is the free volume fraction in a pure polymer at solid state, T is the temperature and R the constant of perfect gases. Ad and Bd are parameters assumed independent from temperature and moisture concentration. This model has been tested successfully in case of systems solvent/polymer with diffusion coefficients highly dependent on the concentration.

In the case of polymers for temperature ranges where the WLF (Williams, Landel and Ferry, 1955) theory for the free volume is valid, Ferry (1961) expresses the Doolittle’s equation for viscosity as a function of free volume and empirical parameters. The effect of increased pressure which induces a fall in the free volume is taken into account by this equation:

ln(ηpη0)=(1vσf−1v0f)	(6)

where 0, p, v0f and vσf are respectively the viscosities and the free volume fractions at atmospheric pressure and under pressure. When the free volume fraction is expressed by the compressibility f which represents the collapse of the free volume, the equation (6) becomes:

ln(ηpη0)=Kfpv0f(v0f−Kfp)	(7)

where p is the pressure.

This result can be used to calculate the diffusion coefficient since  and D are related by the general expression (Fujita, 1961; Ferry, 1961):

ln(DRT)=C−aln(η)	(8)

where C and a are two constants.

From the expressions (6) and (8), we can get a Doolittle-type relationship between the diffusion coefficients at stressed and stress free states D and D0 respectively:

ln(DσD0)=a(1v0f−1vσf)	(9)

This expression is used by Fahmy and Hurt (1980), in the case of polymers and by Neumann and Marom (1985) in the case of composite materials.

In what follows, the process of diffusion in the presence of an external mechanical loading is studied. The application of such a load is expected to modify the microstructure of the material and cause a change in the matrix polymer absorption behavior which becomes dependent on the free volume. Consequently, the cellular diffusion problem is solved on the basis of free volume theory. First, the free volume fraction is determined from the resolution of the mechanical problem imposed on the representative volume element and in a second step the hygroscopic problem is solved. In parallel, the effect of mechanical loading on the diffusion coefficient and on the diffusion parameters is discussed. Finally, on the basis of the results obtained, the coupling effects on the evolution of moisture content are examined.

2. Hygro-mechanical problem

2.1 Mechanical problem

The considered unit cell is composed of two concentric cylinders representing the fiber and matrix constituents (Figure 1). These constituents are assumed homogeneous and in perfect adherence. We denote by rf the radius of the fiber and by rm the matrix one.

rf

rm

Figure.1: representative volume element (RVE).

The determination of the effective hygro-elastic behavior is obtained through solving the cellular problem on RVE on which is imposed an average macroscopic strain E or an average macroscopic stress  and a macroscopic moisture loading Δm. These macroscopic quantities generate local stresses and strains which are solutions of the cellular problem resulting from the following conditions:

- Global force balance of the RVE,

- Hygroelastic behavior in the RVE,

- Compatibility equations in the RVE,

- Stress continuity at the interface,

- Displacement continuity at the interface,

- Macroscopic stress imposed.

‖div(σ(y))=0‖σ=L(y):ε(u)−β(y)Δm‖ε=12(∇u+∇tu) ‖σ(y).n=0 ‖u=0 ‖σ= 	(10)

The notation x denotes the jump of the quantity x at the interface and the notation  indicates the volume average on the RVE. u represents the displacement field solution of cellular problem. L is the elasticity tensor, β is the moisture expansion tensor and Δm the moisture content increment defined by:

Δm=m−m0	(11)

where m is moisture content at time t and m0 is the initial moisture content.

2.2 Calculation of the matrix free volume

To calculate the matrix free volume, first, we must determine the mechanical deformation in the matrix by solving the cellular problem (10). In our case, we use a stress approach in which the macroscopic loading is a traction or a compression imposed on the outer edge of the RVE in the radial direction:

lim σ(y) n =±P er	(12)

The macroscopic stress is written in the form:

σ=1VVEσ(y)dy=Per⊗er	(13)

Due to the cylindrical geometry, the resolution is conducted in a cylindrical coordinate system(er,eθ,ez). We note by (r,θ,z) the variables of this system and by (w,v,u) the corresponding components of the vector displacement. Taking into account the geometry of the problem and the mechanical boundary conditions, the displacement field solution of the problem (10) in each phase is written as follows (Jacquemin et al, 2006):

In the matrix:

u(z)=Amz	 (14)

In the fiber:

u(z)=Afz 	 (15)

The components of the strain tensor are then given by the following expressions:

‖εrr=∂w(r)∂r‖εθθ=w(r)r‖εrθ=εrz=εθz=0‖εzz=∂u(z)∂z	(16)

Finally, the displacement field depends on five unknown constants Af, Bf, Am, Bm and Cm to be determined. These constants are calculated by considering the boundary and continuity conditions at the interfaces.

1 - Continuity of displacement field at the interface fiber / matrix:

uf(rf)=um(rf) 	(17)

2 - Continuity of the radial stress at the interface and hydrostatic pressure applied on the RVE:

σrrf(rf)=σrrm(rf)	(18)

3- Global balance of the RVE:

0rfrσzzfdr+rfrmrσzzmdr=0	(19)

The five coefficients are determined through the five previous equations and the free volume of the matrix is given by the following expression (Neumann and Marom, 1985):

vσf=v0f+(ΔVV0)m 	(20)

v0f and vσfare the volume fractions of free volume at stress free and stressed states, respectively. (ΔVV0)m is the volume strain of the matrix expressed by :

(ΔVV0)m=εrrm+εθθm+εzzm	(21)

3. Effects of mechanical loading on the diffusion parameters

3.1 Effect of mechanical loading on the moisture content at saturation

When the RVE is subjected to a mechanical loading, there is a variation of the free volume of the matrix. The variation of the total volume is attributed to both the matrix and fibers. We assume that the change of volume induces an increase in moisture content capacity. The free volume of the matrix under stress is expressed by (21). The average moisture concentration in the RVE is:

cRVE=(1−vf)cm+vfcf	(22)

where cRVE, cm and cf are the moisture concentrations respectively in the RVE, matrix and fiber, considering the relationship between the moisture content and the moisture concentration:

cα=ραmα	(23)

mRVE=(1−vf)ρmρRVEmm+vfρfρRVEmf	(24)

mRVE  and ρRVE are respectively the moisture content at saturation and the density of the RVE. Under mechanical loading, the expression (24) is written as:

mREVσ=(1−vf)ρmρREVmmσ+vfρfρREVmfσ	(25)

In the case where the fiber is impermeable, we have mf = 0 and the expression (25) becomes:

mRVEσ=(1−vf)ρmρRVEmmσ	(26)

The moisture content in the stressed matrix is:

mmσ=mm0+(ΔV/V0)mρeρm	(27)

with:

mm0=v0fρeρm	(28)

where ρeand ρmare respectively, the water and matrix densities.

The hygroscopic problem resolution provides the transient moisture content evolution in the RVE. The average moisture content at each time is estimated in the matrix by the following expression:

mmoy(τ)=1ζm−ζfζfζmm(τ)dζ 	(29)

where m and f are adimensional radii.

3.2 Effect of mechanical loading on the gap parameters at the interface fiber/matrix

In the case of a permeable fiber in stress free state, the moisture concentration gap  at the interface fiber / matrix is defined as follows:

α=cfcm=mfρfmmρm	(30)

From this expression, the gap parameter  under stress is estimated:

ασ=cfσcmσ=mfσρfmmσρm=ρf[mf+(ΔVV0)fρeρf]ρm[mm+(ΔVV0)mρeρm]	(31)

Simplifications lead to the following expression:

ασ=α+(ΔVV0)fρeρmmm01+(ΔVV0)mρeρmmm0 	(32)

ασ=α+(ΔVV0)fρeρmmm01+(ΔVV0)mρeρmmm0	(32)

ασα0

σ(MPa)

Figure.2: moisture content gap for different mechanical loads (impermeable fiber vf = 0.7).

On the Figure 2 is plotted the evolution of the concentration gap parameter in stress state reported to the gap parameter in stress free state for  tensile or compressive mechanical loads. For the range considered, a slight decrease in gap parameter for tensile loads is observed. Nevertheless, a slight increase in gap parameter for a compressive load is observed. For both types of loading, this variation does not exceed 5%.

ασ

vf

Figure.3: evolution of the gap parameter for different fiber volume fractions.

Figure 3 shows the influence of the fiber volume fraction on the gap parameter for two loading levels. For both loads, this parameter remains almost constant.

3.3 Effect of mechanical loading on the diffusion coefficients

In general, the diffusion coefficients for composite materials with impermeable fibers are often written as follows:Deff=Dmf(vf), where f (vf ) is a function of the fiber volume fraction (Bao and Yee, 2002).

| Model | f(vf) |
| --- | --- |
| Springer-Tsai | f(vf)=1−2vfπ |
| Hashin | f(vf)=1−vf1+vf |
| Woo and Pigott | f(vf)=21−4vfπtan−11+2vfπ1−2vfπ−π2+1−2vfπ−1 |

Table.1: the f(vf) function for several models of diffusion.

By exploiting the expression (9), the relationship between the effective diffusion coefficient of the composite under stress and in stress free state can be expressed:

ln(DeffσDeff)=ln(Dmσf(vf)Dmf(vf))=ln(DmσDm)=a(1v0f−1vσf)	(33)

where a is a constant,v0f and vσf are respectively the free volume fraction under stress free and stressed states. Dm and Dmσ are respectively the diffusion coefficients of the matrix in stress free and stressed states. By introducing the relation (20) between v0f to vσf in (33), we get:

ln(DeffσDeff)=ln(DmσDm)=a(ΔV V0)mv0f[v0f+(ΔVV0)m]	(34)

The effective diffusion coefficient for permeable fibers, in the stress free state, is expressed by (Gueribiz et al, 2009):

DeffprDm=1−vf1+vf+ψ1+ψ1−vf1+vf	(35)

Where ψis related to the gap parameter in stress free state and expressed as:

ψ=αDfDm	(36)

From the expression (34), the diffusion coefficient of the matrix under mechanical loading is given by:

Dmσ=Dmexp(a(ΔV V0)mv0f[v0f+(ΔVV0)m])	(37)

For the composite, we have:

Deffσ=Deffexp(a(ΔV V0)mv0f[v0f+(ΔVV0)m])	(38)

Finally, we obtain the following expressions for the effective diffusion coefficient of composite materials, with permeable fibers, under stress:

Deffpr(σ)=Dmσ1−vf1+vf+ψ1+ψ1−vf1+vf 	(39)

Deffpr(σ)=Dmexp(a(ΔV V0)mv0f[v0f+(ΔVV0)m])1−vf1+vf+ψ1+ψ1−vf1+vf	(40)

The expression (40) shows that the mechanical loading only affects the matrix diffusivity, which is function of the matrix diffusivity in the stress free state and of a mechanical dependent parameter, called Doolittle parameter, defined as:

δDooli=DmσDm=exp(a(ΔV V0)mv0f[v0f+(ΔVV0)m]) 	(41)

The expression (39) becomes:

Deffpr(σ)Dm=δDooli1−vf1+vf+ψ1+ψ1−vf1+vf	(42)

For a compressive load, δDooli<1, the diffusion coefficient is reduced. For a tensile load, δDooli>1, the diffusion coefficient increases as shown in Figure 4.

(a)

(b)

(c)

Figure. 4: effective diffusivity as function of ψ for different mechanical loads: (a) +100 MPa, (b) stress free state, (c) -100 MPa.

ψ

ψ

DeffprDm0

On the other hand, we have:

ψσ=ασDfσDmσ	(43)

Thus:

ψσψ=ασαDfσDfDmDmσ	(44)

Assuming that Dfσ≈Df the expression (44) becomes:

ψσ=ψασαDmDmσ	(45)

Considering (45) and (41), we arrive at the following expression:

ψσ=ψασαexp(−a(ΔV V0)mv0f[v0f+(ΔVV0)m])	(46)

Since the variation of ασwith stress is almost negligible, whatever the fiber volume fraction, the expression (46) becomes:

ψσψ=exp(−a(ΔV V0)mv0f[v0f+(ΔVV0)m])=1δDooli	(47)

Finally, we get:

ln(ψσψ)=−a(ΔV V0)mv0f[v0f+(ΔVV0)m]=−ln(DmσDm)=ln(DmDmσ)=ln(DeffDeffσ)=a(1vσf−1v0f)	(48)

ψσψ

vf

Figure.5: evolution of ψσψ for different stress states.

On Figure 5, the ratio ψσψ is plotted for different stress states and fiber volume fractions. It appears that the ratio is only sensitive to the mechanical loading. This ratio is greater than one for the traction and less than one for compression.

The question that arises now is to express the effective diffusivity under stress according to the permeability indexψσ.

By considering, the expression (47) and (42), we obtain the following expression:

Deffpr(σ)Dmσ=1−vf1+vf+δDooliψσ1+ψσδDooli1−vf1+vf	(49)

The general equation (49) for the diffusivity depends on the loading type. The effect of the mechanical loading state on the diffusivity is summarized in Table 2.

| State | Dooli |  | Deffpr(σ) |
| --- | --- | --- | --- |
| Stress Free State σ=0 | 1 |  | Deffpr |
| Traction σ>0 | >1 | < | Deffpr(σ)>Deffpr |
| Compression σ<0 | <1 | > | Deffpr(σ)<Deffpr |

Table.2: effect of mechanical loading state on the diffusivity.

δDoli=0.001

δDooli=0.001

δDooli=0.02

δDooli=0.12

δDooli=1

δDooli=0.5

δDooli=2.3

δDooli=2

δDooli=1.4

ψσ

Figure.6: effective diffusion coefficient as a function of different stress states (vf = 0.7).

In Figure 6 is presented the effective diffusivity as a function of the parameter  for different mechanical loading expressed by the parameter Dooli.. We note that the starting points correspond to =0, the value of composite materials with impermeable fibers. For tensile loading, expressed by Dooli >1, the difference between the effective diffusivities is not strongly significant.

For compressive loading, expressed by Dooli<1, the coefficients are very sensitive to the stress level whatever the corresponding value for . Dooli is inversely proportional to the compressive stress, the deviation becomes increasingly important with the increase of the compressive stress (decrease of Dooli).

The composite is more sensitive to a compressive loading than a tensile loading. In addition, a compressive load can radically modify the diffusive behavior. By normalizing with the matrix diffusivity at free state, the expression (49) becomes:

Deffpr(σ)Dm0=δDooli1−vf1+vf+ψσδDooli21+ψσδDooli1−vf1+vf 	(50)

The corresponding ratio for impermeable fibers is:

Deffimper(σ)Dm0=δDooli1−vf1+vf 	(51)

In Figure 7 is represented the evolution of the impermeable fiber composite diffusivity for different stress levels. A tensile loading induces higher diffusivities than in the stress free state, thus traction tends to accelerate the process of diffusion (which is not the case for compressive loading). The difference between the diffusivities for different stress levels is most important for the matrix alone (vf =0) and decreases when the fiber volume fraction increases.

vf

Figure.7: effective diffusivity for different stress states for impermeable fiber composite.

4. Hygroscopic problem

The RVE presented in Figure 1 is exposed to a moisture content gradient. In this case, the diffusion occurs in a radial direction and two Fick’s laws are considered since the moisture diffuses through the matrix and the fiber (52).

∂mm∂t=Dmσ∂2mm∂r2+1r∂mm∂r in matrix rf < r<rm t>0  	(52)

Initial, boundary, flux continuity, moisture content discontinuity conditions are given by:

Dmσ∂mm(rf,t)∂r=Df∂mf(rf,t)∂r mf(rf,t)=ασρmρf mm(rf,t) mm(rm,t)=mmσ, 	(53)

where mm is the moisture content at saturation in the matrix, Dm and Df  are the matrix and fiber diffusivities.

By putting ζ=rrm, τ=Dmσrm2t and φ=DfDm, equation (53) becomes a dimensionless equation:

∂mm∂τ=∂2mm∂ζ2+1ζ∂mm∂ζ in matrix ζf < ζ<1 t>0 	(54)

And the initial, boundary, flux continuity, moisture content discontinuity conditions are rewritten as:

∂mm(ζf,τ)∂ζ=φδDoli∂mf(ζf,τ)∂ζ mf(ζf,τ)=ασρmρf mm(ζf,τ) mm(1,τ)=mmσ, 	(55)

For impermeable fibers,  must be taken equal to zero in the preceding equations.

5. Moisture content evaluation

In this section, we attempt to estimate the moisture content for both fiber types. In case of permeable fibers, the parameters used in the moisture content evaluation are estimated by using Rao et al. (1984) immersion data for epoxy/jute fiber composite in distilled water presented in Table 3.

| Diffusion data (T=25°C) | epoxy resin (LY556HT972) | epoxy/jute fiber composite (vf=0.7) |
| --- | --- | --- |
| Moisture content (%) | 3.2 | 8.5 |
| Diffusivity (mm2/s) | 8.3´10-8 | 4.4´10-7 |

Table .3: diffusion data for epoxy/jute fiber composite immersed in distilled water.

To determine the gap parameterα, the expression (30) is used and the moisture content of the fiber is determined from the expression (24) by using the data in Table 3. The value of α is equal to 3.8.

For the parameterφ=DfDm, the value of the jute fiber diffusivity is needed which is evaluated from the expression (35) and (36) for composite diffusivity in stress free state by using the data of Table 3 and the corresponding value ofα. The value of jute fiber diffusivity obtained is Df = 17.32´10-7 mm2 /s, the diffusivity jute fiber value found in the literature is 17.7430´10-7 mm2/s (Aditya and Sinha, 1996) and the relative deviation between the two values is about 2.4%. Finallyφ=21.

In Figure 8 and 9 is plotted the average moisture content for different types of mechanical loading in the case of impermeable and permeable fibers. For both cases, we note an increase in moisture content at saturation for tensile loading which is due to the free volume increase. On the opposite, a decrease takes place for compressive loading condition. As we note, the time to reach saturation is longer for permeable fiber than impermeable fiber, this is quite expected because in this case the diffusion occurs in both the matrix and fiber.

τ=Dmtrm2

mmoy(τ)mVER

MmσMm0

Dtrm

Figure.8: average moisture content for various mechanical loads (impermeable fiber vf = 0.7).

MmσMm0

Dtrm

mmoy(τ)mVER

τ=Dmtrm2

Figure.9: average moisture content for various mechanical loads

MmσMm0

Dtrm

(Permeable fiber vf = 0.7,φ=21,α=3.8).

6. Conclusion

As several experimental studies have shown (Neuman and Marom, 1985, Weitsman, 1987), the proposed modelling confirms that the presence of external mechanical loading has a strong effect on the moisture diffusion process in composites.

By maintaining a Fick’s diffusion behavior, the free volume theory leads to the theoretical interpretation of this behavior. A tensile loading involves an increase in moisture content at saturation and diffusivity and thus accelerates the diffusion process. However, compression may cause a decrease in moisture content at saturation and in diffusivity and thereby slows down the diffusion process.

A more general form of the effective diffusivity expression function of the stress state has been established. This expression enables to determine, as a particular case, the effective diffusivity for free stress state.

References

Aditya, P.K. and Sinha, P.K. (1996). Moisture diffusion in variously shaped fibre reinforced composites, Journal of Computers and Structures, 59: 157-166.

Bao, L.R. and Yee, A.F. (2002). Moisture diffusion and hygrothermal aging in bismaleimide matrix carbon fiber composites-part I: uni-weave composites, Journal of Composite Science and Technology, 62: 2099-2110.

Cohen, M.H. and Turnbull, D. (1959). Molecular transport in liquids and glasses, Journal of Chemistry and Physics, 31: 1164-1169.

Crank, J. and Park, G.S. (1968). Diffusion in polymers, London: Academic press Inc.

Doolittle, A.K. (1951). Studies in Newtonian Flow. II. The Dependence of the Viscosity of Liquids on Free-Space, Journal of Applied Physics, 22: 1471-1475.

Fahmy, A.A. and Hurt, J.C. (1980). Stress Dependence of water diffusion in Epoxy Resins, Journal of polymer composites, 1: 77-88.

Fujita, H. (1961). Diffusion in polymer-diluent systems, Fortschritte der Hochpolymeren-Forschung, 3:1-47.

Ferry, J.D. (1961).  Viscoelastic properties of polymers, John Willey and Sons, Inc.

Gueribiz, D., Jacquemin, F., Rahmani, M., Fréour, S., Guillén, R. and Loucif, K. (2009).  Homogenization of moisture diffusive behaviour of composite materials with impermeable or permeable fibres – Application to porous composite materials, Journal of Composite Materials, 43: 1391-1408.

Jacquemin, F., Fréour, S. and Guillén, R. (2006). Analytical modeling of transient hygro-elastic stress concentration - Application to embedded optical fiber in a non-uniform transient strain field, Journal of Composite Science and Technology, 66: 397-406.

Rao, R.M.V.G.K., Chanda, M. and Balsubramanian, N. (1984). Factors Affecting                                   Moisture Absorption in Polymer Composites Part II: Influence of External Factors, Journal of Reinforced plastic and composites, 3: 246-251.

Weitsman, Y. (1987).  Stress assisted diffusion in elastic and viscoelastic materials, Journal of Mechanical Physics Solids, 35: 73-93.

Williams, M.L., Landel, R.F. and Ferry J.D. (1955). The temperature dependence of relaxation mechanisms in amorphous polymers and other glass-forming liquids, Journal of the American Chemical Society, 77: 3701-3707.